# MH Photoluminescent pigment

(Long afterglow glow in the dark powder)

| ## Model | ## Size （um） | AFTERGLOW INTENSITY（mcd/㎡） |  |  |  |  | FOB Price (USD/KG) | ## Glowing color （Night） | ## Appearance （Daytime） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 min | 5 min | 30 min | 60 min | Glow time |  |  |  |
| #### MHG-4B | 65~75 | 3756 | 1231 | 243 | 115 | >12hr | 34 | Yellow-green | Light-yellow |
| MHG-4C | 45~55 | 3282 | 997 | 173 | 78 |  | 34 |  |  |
| MHG-4D | 25~35 | 2300 | 650 | 120 | 52 |  | 34 |  |  |
| MHG-4E | 5~15 | 1130 | 320 | 55 | 28 |  | 35 |  |  |
| MHG-4CY | 45~55 | 1452 | 410 | 70 | 36 | 8hr | 38 |  |  |
| MHG-4DY | 25~35 | 1100 | 315 | 53 | 27 |  | 38 |  |  |
| MHG-5C | 45~55 | 3610 | 947 | 160 | 70 |  | 38 |  |  |
| MHG-5D | 25~35 | 2530 | 610 | 110 | 46 |  | 38 |  |  |
| MHG-2C | 55~75 | 2187 | 658 | 108 | 45 |  | 20 |  |  |
| MHG-2D | 15~40 | 1542 | 470 | 85 | 34 |  | 20 |  |  |
| MHG-1D | 15~45 | 1387 | 380 | 60 | 26 |  | 14 |  |  |
| MHB-4B | 65~75 | 2976 | 1104 | 225 | 120 | >12hr | 34 | Blue-green | Light-yellow |
| MHB-4C | 45~55 | 2340 | 832 | 169 | 91 |  | 34 |  |  |
| MHB-4D | 15~35 | 1580 | 570 | 108 | 57 |  | 34 |  |  |
| MHB-3C | 55~75 | 1800 | 550 | 110 | 58 | 8hr | 20 |  |  |
| MHB-3D | 15~40 | 1380 | 470 | 90 | 38 |  | 20 |  |  |
| MHBW-4D | 15~35 | 1400 | 500 | 92 | 45 |  | 34 | Blue-green | White |
| MHP-6C | 45~55 | 720 | 250 | 30 | 13 | 3hr | 25 | purple | White |
| MHP-6D | 15~45 | 480 | 165 | 21 | 9 |  | 25 |  |  |
| MHSB-8D | 15~50 | 980 | 300 | 31 | 15 | 6hr | 25 | Blue | White |

##### Photoluminescent sand

| ## Model | ## Size （mm） | AFTERGLOW INTENSITY（mcd/㎡） |  |  |  |  | FOB Price (USD/KG) | ## Glowing color （Night） | ## Appearance （Daytime） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 min | 5 min | 30 min | 60 min | Glow time |  |  |  |
| MHG-4A | 0.5~2 | 6400 | 1900 | 290 | 120 | >12hr | 34 | Yellow-green | Light-yellow |
| #### MHG-4BA | 0.15-0.3 | 6400 | 1900 | 290 | 120 |  |  |  |  |
| MHG-2A | 0.5~2 | 2187 | 658 | 108 | 45 |  | 20 |  |  |
| MHG-2BA | 0.15-0.3 | 2187 | 658 | 108 | 45 |  |  |  |  |
| MHB-4A | 0.5~2 | 3580 | 1250 | 250 | 120 |  | 34 | Blue-green | Light-yellow |
| MHB-4BA | 0.15-0.3 | 3580 | 1250 | 250 | 120 |  |  |  |  |

MH series: This series photoluminescent pigment is made of alkaline earth aluminate. The chemical formula: AlxSryCa(1-y)Oz: Eu Dy

# MS Photoluminescent pigment

(sulphide Photoluminescent pigment)

| ## Model | ## Size （um） | AFTERGLOW INTENSITY（mcd/㎡） |  |  |  |  | FOB Price (USD/KG) | ## Glowing color （Night） | ## Appearance （Daytime） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 min | 5 min | 30 min | 60 min | Glow time |  |  |  |
| ###### MSGG-4D | 10~30 | 500 | 89 | 10 | 4 |  | 17 | Yellow-green | Yellow |
| MSRR-4D | 20~50 | 400 | 50 | 2.5 | 1 | >1hr | 70 | Red | red |
| MSRO-4D | 20~50 | 400 | 50 | 2.5 | 1 |  | 70 | Red | Orange |
| MSWW-4D | 15~45 | 900 | 300 | 54 |  | >6hr | 68 | White | White |
| MSWO-4D | 10~45 | 460 | 60 | 3.2 | 1.1 | >6hr | 115 | Orange | White |

# MS series: It is sulfide Photoluminescent material. The chemical formula: MxOySz:Eu Ln or ZnS:Cu.

# MT Photoluminescent pigment

(Daytime Appearance: neon color)

| ## Model | ## Size （um） | AFTERGLOW INTENSITY（mcd/㎡） |  |  |  |  | FOB Price (USD/KG) | ## Glowing color （Night） | ## Appearance （Daytime） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 min | 5 min | 30 min | 60 min | Glow time |  |  |  |
| MTR-4D | 25~35 | 1050 | 300 | 55 | 26 | >6hr | 20 | Orange-Red | red |
| MTG-4D | 25~35 | 945 | 270 | 50 | 24 |  | 20 | Green | Green |
| MTY-4D | 25~35 | 1200 | 345 | 62 | 28 |  | 20 | Yellow | Yellow |
| MTO-4D | 25~35 | 1050 | 300 | 55 | 26 |  | 20 | Orange | Orange |
| MTB-4D | 25~35 | 700 | 230 | 45 | 20 |  | 20 | Blue | Blue |

##### MT series: This series Photoluminescencet pigment by dyeing process on base of MH series.

Remarks: price are valid before 2009-03-30

- Measurement according to Din 67 510 Part 1

- The MHG-4CY and MHG-4DY is rapid excited photoluminescent pigment. The tested in conditions:36W fluorescent light for laser illuminant,150Lx for lighting intensity for 15 min running.

- To pay USD3.50/kg extra on MH type powders above for encapsulated for water based application(MH-W).

- Normal packing: 1kg each plastic or 25 kgs each plastic pail.

- We can accept OEM based on customers' sample or customers’ technology reference data sheet.

Contact Person: Mike Xu

### Lanxi Minhui Photoluminescent Co., Ltd

Http://www.mphotoluminescent.com    E-mail:sales@mphotoluminescent.com

MSN: glow_mikexu@hotmail.com   TEL:86-579-88948789;88948900     FAX:86-579-88948948